KEYAN Calculation — Technical Support Documentation

Core Simulation Setup & Load Case Configuration Guide

1. Multiphysics Load Case & Workflow Architecture

For complex structural-thermal industrial applications, such as CO2 shielded welding, additive manufacturing, and thermal cladding, a Sequentially Coupled Thermal-Structural analysis approach is mandated. The simulation pipeline isolates the thermal physics from the stress field physics to maximize computational stability while maintaining non-linear precision.

Transient Thermal Stage: Calculates the time-dependent temperature field history under highly localized, moving heat fluxes. Convection and radiation boundary conditions are active and updated at every sub-step.

Static Structural Stage: Imports the complete 4D (Spatial + Temporal) temperature profile as a thermal body load. Calculates thermal expansion, plastic strain development, and cumulative structural residual deformations.

2. Advanced Thermal Boundary Conditions & Heat Source Setup

To accurately capture the intense localized heat input from welding or lasers, a moving heat flux distribution must be established. KEYAN Calculation standardizes on the Goldak Gaussian Double-Ellipsoidal Heat Source Model.

The heat generation density distributions for the front (f) and rear (r) quadrants of the moving weld pool are defined via the following equations:

q_f(x,y,z,t) = [ 6 * sqrt(3) * f_f * Q ] / [ a * b * c_f * pi * sqrt(pi) ] * exp( -3*x^2/a^2 - 3*y^2/b^2 - 3*(z - v*t)^2/c_f^2 )

q_r(x,y,z,t) = [ 6 * sqrt(3) * f_r * Q ] / [ a * b * c_r * pi * sqrt(pi) ] * exp( -3*x^2/a^2 - 3*y^2/b^2 - 3*(z - v*t)^2/c_r^2 )

Where: Q = Total Effective Power (W) = Efficiency (eta) * Voltage (V) * Current (I); v = Welding Velocity (mm/s); a, b, c_f, c_r are the melt pool geometric parameters, and f_f + f_r = 2.0 represent the fractional energy distributions.

Environmental dissipation settings must be modeled simultaneously using the following parameters:

| Dissipation Type | Boundary Implementation | Standard Quantitative Value |
| --- | --- | --- |
| Surface Convection | Newtonian Cooling Face Effect | h = 15.0 – 25.0 W/(m²·°C) (Ambient Air) |
| Surface Radiation | Stefan-Boltzmann Emissivity Surface | Epsilon = 0.80 – 0.85 (Structural Carbon Steels) |

3. Mechanical Boundary Conditions & Fixture Constraints

To properly capture industrial welding clamps and anti-deformation fixtures, mechanical constraints must not over-constrain the structural components, which causes false artificial stress spikes.

Primary Reference Clamps: Apply Fixed Supports only to realistic localized fixture contact locations. Avoid locking the entire bottom face unless the structure is continuously welded to a thick baseplate.

Elastic Tooling Supports: For temporary or spring-loaded manufacturing clamps, utilize Elastic Foundation boundary settings with stiffness values matching the physical hydraulic or mechanical clamp properties.

4. Non-Linear Solver Tuning & Convergence Settings

Extreme temperature variations (up to 2200°C) introduce severe material non-linearity, which often triggers solver divergence. The following settings are required for the Newton-Raphson iterative solver:

Time-Step Control (Auto Time Stepping): Must be set to ON. During active heat input periods, define the initial time-step as 0.05s, minimum time-step as 0.001s, and maximum time-step as 0.2s to track peak gradients smoothly.

Large Deflection Effects: Must be toggled ON in the static structural solver options to account for geometric stiffness changes induced by thin sheet-metal warping and buckling behaviors.

Non-Linear Stabilization: Activate energy-based stabilization factors (e.g., Constant Damping factor = 1e-4) if localized macro-buckling causes momentary structural instability during the intermediate cooling stages.

CRITICAL CONFIGURATION NOTICE: The moving velocity parameter v must match the true physical weld tracker feed rate. Deviations in time-step sizing relative to mesh density will result in spatial numerical oscillation and false temperature peaks. For custom user subroutines (DFLUX/APDL), contact support@keyan-calculation.com.